Technical Data Sheet

Bergamid™ B80 Black Polyamide 6

Key Characteristics

Product Description

PA6 compound

General

Material Status • Commercial: Active

Regional Availability • Asia Pacific

Appearance • Black

Processing Method • Injection Molding

Technical Properties 1

Physical Typical Value (English) Typical Value (SI) Test Method

Specific Gravity 1.13 1.13 ASTM D792

Molding Shrinkage 1.2 to 1.6 % 1.2 to 1.6 % ASTM D955

Mechanical Typical Value (English) Typical Value (SI) Test Method

Tensile Strength 2 10900 psi 75.0 MPa ASTM D638

Flexural Modulus 3 377000 psi 2600 MPa ASTM D790

Flexural Strength 3 14500 psi 100 MPa ASTM D790

Impact Typical Value (English) Typical Value (SI) Test Method

Notched Izod Impact ASTM D256

73°F (23°C), 0.126 in (3.20 mm) 0.56 ft·lb/in 30 J/m

Thermal Typical Value (English) Typical Value (SI) Test Method

Deflection Temperature Under Load ASTM D648

264 psi (1.8 MPa), Unannealed, 0.126 in

(3.20 mm) 149 °F 65.0 °C

Electrical Typical Value (English) Typical Value (SI) Test Method

Surface Resistivity > 1.0E+12 ohms > 1.0E+12 ohms ASTM D257

Flammability Typical Value (English) Typical Value (SI) Test Method

Flame Rating (0.13 in (3.2 mm)) HB HB Internal Method

Processing Information

Injection Typical Value (English) Typical Value (SI)

Drying Temperature 176 to 194 °F 80.0 to 90.0 °C

Drying Time 2.0 to 4.0 hr 2.0 to 4.0 hr

Processing (Melt) Temp 464 to 536 °F 240 to 280 °C

Mold Temperature 149 to 185 °F 65.0 to 85.0 °C

Injection Notes

Injection Pressure: MED-HIGH

Hold Pressure: MED-HIGH

Screw Speed: MODERATE

Back Pressure: LOW

Notes

1 Typical values are not to be construed as specifications.

2 2.0 in/min (50 mm/min)

3 0.051 in/min (1.3 mm/min)

Copyright ©, 2016 PolyOne Corporation. PolyOne makes no representations, guarantees, or warranties of any kind with respect to the Information contained in this document about its

accuracy, suitability for particular applications, or the results obtained or obtainable using the information. Some of the Information arises from laboratory work with small-scale equipment which

may not provide a reliable indication of performance or properties obtained or obtainable on larger-scale equipment. Values reported as “typical” or stated without a range do not state minimum

or maximum properties; consult your sales representative for property ranges and min/max specifications. Processing conditions can cause material properties to shift from the values stated in

the Information. PolyOne makes no warranties or guarantees respecting suitability of either PolyOne’s products or the Information for your process or end-use application. You have the

responsibility to conduct full-scale end-product performance testing to determine suitability in your application, and you assume all risk and liability arising from your use of the Information

and/or use or handling of any product. POLYONE MAKES NO WARRANTIES, EXPRESS OR IMPLIED, INCLUDING, BUT NOT LIMITED TO, IMPLIED WARRANTIES OF

MERCHANTABILITY AND FITNESS FOR A PARTICULAR PURPOSE, either with respect to the Information or products reflected by the Information. This data sheet shall NOT operate as

permission, recommendation, or inducement to practice any patented invention without permission of the patent owner.

Rev: 2014-07-23