| QMFZ2 Component - Plastics |  | Friday, November 21, 2003 |  |  |  |  |  |  | E41938 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| E I DUPONT DE NEMOURS & CO INC ENGINEERING POLYMERS CHESTNUT RUN PLAZA PO BOX 80713 WILMINGTON DE 19880 |  |  |  |  |  |  |  |  |  |
| Material Designation: SK601 |  |  |  |  |  |  |  |  |  |
| Product Description: Polybutylene Terephthalate (PBT), glass reinforced, designated "Crastin" furnished as pellets. |  |  |  |  |  |  |  |  |  |
| Color | Min. Thick. (mm) | Flame Class | HWI | HAI | RTI Elec | RTI Imp | RTI Str | IEC GWIT | IEC GWFI |
| ALL | 0.75 | - | - | - | 130 | 115 | 120 | - | - |
|  | 1.5 | HB | 3 | 1 | 130 | 115 | 120 | - | - |
|  | 3.0 | HB | 3 | 1 | 130 | 115 | 120 | - | - |
|  | 6.0 | HB | 1 | 1 | 130 | 115 | 120 | - | - |
| CTI: 2 | IEC CTI (V): - | HVTR: 1 |  |  | D495: 6 |  |  | IEC Ball Pressure (°C): - |  |
| Dielectric Strength (kV/mm): 35 ISO Tensile Strength (MPa): - ISO Tensile Impact (kJ/m2): - |  | Volume Resistivity (10xohm-cm): 16 ISO Flexural Strength (MPa): - ISO Izod Impact (kJ/m2): - |  |  |  |  |  | Dimensional Stability(%): 0 ISO Heat Deflection (°C): - ISO Charpy Impact (kJ/m2): - |  |
| NOTE | (1) Material designations that are color pigmented may be followed by suffix letters and numbers. (2) Material designations may be prefixed by "ZYT" or "MIN" or "ZEN" or "DEL" or "CRA" or "RYN". |  |  |  |  |  |  |  |  |
| Report Date: 1/17/1996 |  | Underwriters Laboratories Inc® |  |  |  |  |  |  |  |
| UL94 small-scale test data does not pertain to building materials, furnishings and related contents. UL 94 small-scale test data is intended solely for determining the flammability of plastic materials used in components and parts of end-product devices and appliances, where the acceptability of the combination is determined by ULI. |  |  |  |  |  |  |  |  |  |